## Slide 1: Technical Programme on "SOIL MECHANICS, FOUNDATION ENGINEERING & GEOTECHNICAL INVESTIGATIONS RELATED TO ELECTRIC SUB-STATION, EXTRA HIGH TENSION TRANSMISSION LINES AS PER QC, QA WITH IEC CONFORMITY" for Engineers of APTRANSCO (Civil, Electrical & Telecom) at Training institute, APGENCO, Ibrahimpatnam
Dr. G. V. RAMA SUBBARAO
ASSOCIATE PROFESSOR,
DEPARTMENT OF CIVIL ENGINEERING,
V.R. SIDDARTHA SCHOOL OF ENGINNERING,
SIDDHARTHA ACADEMY OF HIGHER EDUCATION
-Deemed to be University
VIJAYAWADA – 520 007
E-Mail: drgeovrs@vrsiddhartha.ac.in
Civil@VRS - YouTube

## Slide 2
Introduction to Soil Mechanics & Foundation Engineering
Soil Stress & Deformation
Soil Strength
Foundation Types
Foundation Design
Earth Retaining Structures
Geotechnical Investigations
Construction Aspects
Case studies & examples, Successful foundation design
Extracts of important Indian Standards as per QC,QA with IEC conformity
CONTENTS

## Slide 3
Modern Geotechnical Engineering

## Slide 4
Introduction to
SOIL MECHANICS & FOUNDATION ENGINEERING
[GEOTECHNICAL ENGINEERING ]
Geotechnical engineering in an applied science dealing with the applications or principles of soil mechanics to practical problems.
It has a much wider scope than soil mechanics, as it deals with all engineering problems related with soils.
It includes site investigations, design and construction of foundations, earth-retaining Structures and earth structures.

## Slide 7
Unfortunately, soils are made by nature and not by man, and the products of nature are always complex.
Karl von Terzaghi, 1936

## Slide 10
“Geotechnical Engineering” by Dr. C. Venkatramaiah - A comprehensive textbook covering various aspects of geotechnical engineering, including soil mechanics, foundation engineering, and ground improvement techniques.
“Soil Mechanics and Foundation Engineering” by Dr. K. R. Arora - A widely used textbook in Indian engineering universities, covering fundamental principles of soil mechanics and foundation engineering, with a focus on practical applications.
“Soil Mechanics and Foundation Engineering” by Dr. V. N. S. Murthy. “Foundation Engineering” by Dr. P. C. Varghese. “Advanced Foundation Engineering: Geotechnical Engineering Series” by Dr. V. N. S. Murthy

## Slide 13: Typical Geotechnical Project
construction site
Geo-Laboratory ~ for testing
Design Office ~ for design & analysis
soil samples
soil properties
design details

## Slide 15
Sieve analysis – for coarse grain soils
Classify coarse by GSD and
fines from Atterberg limits (PI-LL chart)

## Slide 16: Grain Size Distribution
In coarse grain soils …... By sieve analysis
Determination of GSD:
Sieve Analysis
stack of sieves
sieve shaker

## Slide 28
“GRAVEL+SAND”
DESIGN MIX
Case study

## Slide 29
Gravel
Sand

## Slide 30
DESIGN a GRAVEL+ (?%) SAND MIX which having
Plasticity Index (PI)<6%

## Slide 31
Sieve Analysis of Gravel

## Slide 32
Sieve Analysis of Gravel

## Slide 34
Sieve Analysis of Sand

## Slide 37
Liquid Limit Test

## Slide 38
Plastic Limit Test

## Slide 42
Chart: Gravel alone
| 45 | 15
 | 30.772 | 31.455
LIQUID LIMIT |  |  |  | 
Number of blows | 45 | 15 |  | 
Container number | 5 | 19 |  | 
Weight of container, g | 13.27 | 13.62 |  | 
Weight of container + Wet soil, g | 49.69 | 47.68 |  | 
Weight of container + Oven dry soil, g | 41.12 | 39.53 |  | 
Weight of water, g | 8.57 | 8.15 |  | 
Weight of oven dry soil, in g | 27.85 | 25.91 |  | 
Water content (%) | 30.77 | 31.46 |  | 
PLASTIC LIMIT |  |  |  | 
Container number | 35 |  |  | 
Weight of container, g | 14.03 |  |  | 
Weight of container + Wet soil, g | 45.07 |  |  | 
Weight of container + Oven dry soil, g | 39.64 |  |  | 
Weight of water, g | 5.43 |  |  | 
Weight of oven dry soil, in g | 25.61 |  |  | 
Water content (%) | 21.2 |  |  | 21.2
PLASTICITY INDEX (PI) (%) |  |  |  | 10.04

## Slide 43
LIQUID LIMIT |  |  |  | 
Number of blows | 40 | 17 |  | 
Container number | 12 | 15 |  | 
Weight of container, g | 13.55 | 12.95 |  | 
Weight of container + Wet soil, g | 48.67 | 43.51 |  | 
Weight of container + Oven dry soil, g | 40.77 | 36.4 |  | 
Weight of water, g | 7.9 | 7.11 |  | 
Weight of oven dry soil, in g | 27.22 | 23.45 |  | 
Water content (%) | 29.02 | 30.32 |  | 
Chart: Gravel + 10% Sand
| 40 | 17
 | 29.0228 | 30.3198
PLASTIC LIMIT |  |  |  |  | 
Container number |  | 1 |  |  | 
Weight of container, g |  | 14.19 |  |  | 
Weight of container + Wet soil, g |  | 43.76 |  |  | 
Weight of container + Oven dry soil, g |  | 38.43 |  |  | 
Weight of water, g |  | 5.33 |  |  | 
Weight of oven dry soil, in g |  | 24.24 |  |  | 
Water content (%) |  | 21.99 |  | 21.99 | 
PLASTICITY INDEX (PI) (%) |  |  |  | 7.9 | 

## Slide 44
LIQUID LIMIT |  |  |  |  | 
Number of blows | 15 | 20 | 25 |  | 
Container number | 6 | 17 | 21 |  | 
Weight of container, g | 12.87 | 14.62 | 13.22 |  | 
Weight of container + Wet soil, g | 48.66 | 50.53 | 52.87 |  | 
Weight of container + Oven dry soil, g | 41.26 | 42.97 | 44.5 |  | 
Weight of water, g | 7.4 | 7.56 | 8.37 |  | 
Weight of oven dry soil, in g | 28.39 | 28.35 | 31.28 |  | 
Water content (%) | 26.07 | 26.67 | 26.76 |  | 
Chart: Gravel + 20% Sand
| 15 | 20 | 25
 | 26.0655 | 26.6667 | 26.7583
PLASTIC LIMIT |  |  |  |  | 
Container number |  | 34 |  |  | 
Weight of container, g |  | 13.94 |  |  | 
Weight of container + Wet soil, g |  | 42.68 |  |  | 
Weight of container + Oven dry soil, g |  | 37.45 |  |  | 
Weight of water, g |  | 5.23 |  |  | 
Weight of oven dry soil, in g |  | 23.51 |  |  | 
Water content (%) |  | 22.25 |  | 22.25 | 

## Slide 45
% of Sand Added | Liquid Limit, LL (%) | Plastic Limit, PL (%) | Plasticity Index, PI =(LL-PL) (%)
0 | 31.24 | 21.2 | 10.04
10 | 29.87 | 22 | 7.882
20 | 26.84 | 22.3 | 4.589

## Slide 46
Chart: PI vs % Sand added to Gravel
| 0 | 10 | 20
Soil-1 | 10.0373 | 7.8816 | 4.5891

## Slide 49
16% of Sand to be added to Gravel
CONCLUSION

## Slide 52
COMPACTION OF SOILS

## Slide 55
Moisture content (%)
Fig. Standard Proctor Compaction Curve
LABORATORY STANDARD PROCTOR COMPACTION TEST
Dry Density (g/cc)
OMC
MDD

## Slide 57
Degree of Compaction or Relative Compaction (%)

## Slide 58
FIELD COMPACTION CONTROL
Testing for Construction of Vehicle shed for Zonal office building at 220KV SS Gunadala
@
TRANSCO NILAYAM, Gunadala, Vijayawada
For
Civil Survey Sub-division,
TRANSMISSION CORPORATION OF ANDHRA PRADESH
Date: 4-1-2014
Case study

## Slide 59
TRANSCO NILAYAM, Gunadala, Vijayawada

## Slide 60
Filled up Soil for Constructing Parking Shed

## Slide 61
Roller used for Compaction

## Slide 63
Determination of
Field (in-situ) Density of Soil
by
Sand Replacement Method

## Slide 70
REPORTING TEST RESULTS

## Slide 71
DETERMINATION OF DENSITY OF COMPACTED LAYER BY SAND REPLACEMENT METHOD | 
Description | Sample
DETERMINATION OF BULK DENSITY OF SAND: | 
Diameter of calibration cylinder D (in cm) | 10
Height of calibration cylinder H (in cm) | 15
Volume of calibration cylinder =(3.14/4*D2*H) (in cc) | 1177.50
Weight of cylinder + Sand W1 (in g) | 6420
Weight of cylinder + Sand W2 (Kept on flat surface) (in g) | 6090
Weight of cylinder + Sand W3 (Kept on Calibration cylinder) (in g) | 4130
Weight of sand in conical portion only Wcp (in g) | 330
Weight of sand in calibration Cylinder & conical portion Wccp (in g) | 1960
Weight of sand in calibration cylinder only Wcc (in g) | 1630
Density of sand ﻻsand = | 1.38
FIELD OBSERVATIONS: | 
Weight of cylinder + Sand W4 (in g) | 6060
Weight of cylinder + Sand W5 (Kept on pit) (in g) | 4765
Weight of excavated soil W6 (in g) | 1435
Weight of sand pit & conical portion Wpcp (in g) | 1295
Weight of sand pit only Wpit (in g) | 965
Volume of pit Vpit (in cc) | 697.11
Field Density (in g/cc) | 2.06
Container number | 26
Weight of container, g | 14.49
Weight of container + Wet soil, g | 52.9
Weight of container + Oven dry soil, g | 48.07
Weight of water, g | 4.83
Weight of oven dry soil, in g | 33.58
Field Moisture content (%) | 14.383562
Field Dry Density, FDD (in g/cc) | 1.7996484
Maximum Dry Density, MDD (in g/cc) from Lab (IS:2720-Part 8) | 1.838
OMC (%) | 15.6
Degree of Compaction (%) = (FDD/MDDx100) | 97.913405

## Slide 72
Soil Strength
SHEAR STRENGTH OF SOILS
Soils are essentially frictional materials
  the strength depends on the applied stress
Strength is controlled by effective stresses
  water pressures are required
Soil strength depends on drainage

## Slide 73: Shear failure
Soils generally fail in shear
strip footing
embankment
At failure, shear stress along the failure surface reaches the shear strength.
failure surface
mobilised shear resistance

## Slide 74: Shear failure
The soil grains slide over each other along the failure surface.
No crushing of individual grains.
failure surface

## Slide 75: Shear failure



At failure, shear stress along the failure surface () reaches the shear strength (f).

## Slide 76: Mohr-Coulomb failure criterion
The limiting shear stress (soil strength) is given by
t = c + sn tan f
where c = cohesion (apparent)
f = friction angle
t
sn

## Slide 77: Mohr-Coulomb Failure Criterion


c

failure envelope
cohesion
friction angle
f is the maximum shear stress the soil can take without failure, under normal stress of .
f


## Slide 78: Mohr-Coulomb Failure Criterion
Shear strength consists of two components: cohesive and frictional.
f
f



c
f tan 
c
cohesive component
frictional component

## Slide 79
c and  are measures of shear strength.
Higher the values, higher the shear strength.

## Slide 80
Mohr-Coulomb criterion (Principal stresses)
t
s
f
s1
s3
c
c cot f
p
R
Failure occurs if a Mohr circle touches the failure criterion. Then
R = sin f ( p + c cot f )

## Slide 81
Mohr-Coulomb criterion (Principal stresses)
t
s
f
s1
s3
c
c cot f
p
R
Failure occurs if a Mohr circle touches the failure criterion. Then
R = sin f ( p + c cot f )

## Slide 82
Mohr-Coulomb criterion (Principal stresses)
t
s
f
s1
s3
c
c cot f
p
R
Failure occurs if a Mohr circle touches the failure criterion. Then
R = sin f ( p + c cot f )

## Slide 83
1- 3 Relation at Failure
X
soil element at failure
3
1
X
3
1

## Slide 84
Effective stress failure criterion
are known as the effective (or drained) strength parameters.
If the soil is at failure the effective stress failure criterion will always be satisfied.

## Slide 85
Effective stress failure criterion
are known as the effective (or drained) strength parameters.
Soil behaviour is controlled by effective stresses, and the effective strength parameters are the fundamental strength parameters. But they are not necessarily soil constants.
If the soil is at failure the effective stress failure criterion will always be satisfied.

## Slide 86
Total stress failure criterion
If the soil is taken to failure at constant volume (undrained) then the failure criterion can be written in terms of total stress as
cu and fu are known as the undrained strength parameters

## Slide 87
Total stress failure criterion
If the soil is taken to failure at constant volume (undrained) then the failure criterion can be written in terms of total stress as
cu and fu are known as the undrained strength parameters
These parameters are not soil constants, they depend strongly on the moisture content of the soil.

## Slide 88
Total stress failure criterion
If the soil is taken to failure at constant volume (undrained) then the failure criterion can be written in terms of total stress as
cu and fu are known as the undrained strength parameters
These parameters are not soil constants, they depend strongly on the moisture content of the soil.
The undrained strength is only relevant in practice to clayey soils that in the short term remain undrained. Note that as the pore pressures are unknown for undrained loading the effective stress failure criterion cannot be used.

## Slide 89
Mohr Circles & Failure Envelope
X
Y
Soil elements at
different locations
X
Y
X
Y
~ failure
~ stable



## Slide 90
Mohr Circles & Failure Envelope
Y
Initially, Mohr circle is a point
c
c
c

c+

The soil element does not fail if the Mohr circle is contained within the envelope
GL

## Slide 91
Mohr Circles & Failure Envelope
Y
c
c
c

GL
As loading progresses, Mohr circle becomes larger…
.. and finally failure occurs when Mohr circle touches the envelope

## Slide 92
Orientation of Failure Plane
Y
c
c
c

GL
c+
90+

45 + /2
Failure plane oriented at 45 + /2 to horizontal
45 + /2
Y

## Slide 93
Envelopes in terms of  & ’
Identical specimens initially subjected to different isotropic stresses (c) and then loaded axially to failure
c
c
c
c
f
Initially…
Failure
uf
At failure,
3 = c; 1 = c+f
3’ = 3 – uf ; 1’ = 1 - uf
c, 
c’, ’
in terms of 
in terms of ’

## Slide 94
Tests to measure soil strength
1. Shear Box Test
Motor drive
Load cell to measure Shear Force
Normal load
Rollers
Soil
Porous plates
Top platen
Measure relative horizontal displacement, dx
vertical displacement of top platen, dy

## Slide 96
Usually only relatively slow drained tests are performed in shear box apparatus. For clays rate of shearing must be chosen to prevent excess pore pressures building up. For sands and gravels tests can be performed quickly
Tests on sands and gravels are usually performed dry. Water does not significantly affect the (drained) strength.
If there are no excess pore pressures and as the pore pressure is approximately zero the total and effective stresses will be identical.
The failure stresses thus define an effective stress failure envelope from which the effective (drained) strength parameters c’, f’ can be determined.
Shear box test

## Slide 97
Typical drained shear box results
t = F/A
s = N/A
Peak
Ultimate
N1
N2

## Slide 98
Tests to measure soil strength
2. The Triaxial Test
Cell pressure
Pore pressure and volume change
Rubber membrane
Cell water
O-ring seals
Porous filter disc
Confining cylinder
Deviator load
Soil

## Slide 99
Stresses in triaxial specimens
sr
sr = Radial stress (cell pressure)
sa = Axial stress
F = Deviator load
sr

## Slide 100
Stresses in triaxial specimens
sr
sr = Radial stress (cell pressure)
sa = Axial stress
F = Deviator load
sr
From equilibrium we have

## Slide 101: Triaxial Test Apparatus
porous stone
impervious membrane
piston (to apply deviatoric stress)
O-ring
pedestal
perspex cell
cell pressure
back pressure
pore pressure or
volume change
water
soil sample at failure
failure plane

## Slide 102: Types of Triaxial Tests
Under all-around cell pressure c
Shearing (loading)
Is the drainage valve open?
Is the drainage valve open?
deviatoric stress ()
yes
no
yes
no
Consolidated sample
Unconsolidated sample
Drained loading
Undrained loading

## Slide 103: Types of Triaxial Tests
Depending on whether drainage is allowed or not during
initial isotropic cell pressure application, and
shearing,
there are three special types of triaxial tests that have practical significances. They are:
Consolidated Drained (CD) test
Consolidated Undrained (CU) test
Unconsolidated Undrained (UU) test

## Slide 104
Granular soils have no cohesion.
c = 0 & c’= 0
For normally consolidated clays, c’ = 0 & c = 0.
For unconsolidated undrained test, in terms of total stresses, u = 0

## Slide 105
There are many test variations. Those used most in practice are:
UU (unconsolidated undrained) test.
Cell pressure applied without allowing drainage. Then keeping cell pressure constant increase deviator load to failure without drainage.
CIU (isotropically consolidated undrained) test.
Drainage allowed during cell pressure application. Then without allowing further drainage increase q keeping sr constant as for UU test.
CID (isotropically consolidated drained) test
Similar to CIU except that as deviator stress is increased drainage is permitted.
Types of triaxial test

## Slide 106
Specimens are subjected to (approximately) uniform stresses and strains
The complete stress-strain-strength behaviour can be investigated
Drained and undrained tests can be performed
Pore water pressures can be measured in undrained tests, allowing effective stresses to be determined
Different combinations of cell pressure and axial stress can be applied
Advantages of the triaxial test

## Slide 107
Mohr Circles
To relate strengths from different tests we need to use some results from the Mohr circle transformation of stress.
t
s
s1
s3

## Slide 108
Mohr Circles
To relate strengths from different tests we need to use some results from the Mohr circle transformation of stress.
t
s
s1
s3
c
The Mohr-Coulomb failure locus is tangent to the Mohr circles at failure

## Slide 109
Effective stress Mohr-Coulomb criterion
As mentioned previously the effective strength parameters are the fundamental parameters. The Mohr-Coulomb criterion must be expressed in terms of effective stresses

## Slide 110
Effective stress Mohr-Coulomb criterion
As mentioned previously the effective strength parameters are the fundamental parameters. The Mohr-Coulomb criterion must be expressed in terms of effective stresses

## Slide 111
Effective stress Mohr-Coulomb criterion
As mentioned previously the effective strength parameters are the fundamental parameters. The Mohr-Coulomb criterion must be expressed in terms of effective stresses
where

## Slide 116
Case study

## Slide 127: Conducting UCC Test to evaluate “Safe Bearing Capacity (qs)”

## Slide 133
Initial diameter of soil specimen, D0 (in cm) | 3.8 |  |  |  |  | 
Initial length of soil specimen, L0 (in cm) | 7.6 |  |  |  |  | 
Initial area of soil specimen, A0 = pi/4*D2 (in cm2) | 11.34262 |  |  |  |  | 
Test Result: |  |  |  |  |  | 
Deformation Dial Reading | 0 | 400 | 500 | 570 | 575 | 585
Change in length of soil sample [Axial deformation, DL] (in mm) | 0 | 4 | 5 | 5.7 | 5.75 | 5.85
Axial strain (e) = [DL/L*100] (in %) | 0 | 5.263158 | 6.578947 | 7.5 | 7.565789 | 7.697368
Corrected area at failure Ac = A0/(1-e) (in cm2) | 11.105 | 11.72194 | 11.88704 | 12.00541 | 12.01395 | 12.03108
Proving ring dial reading | 0 | 3 | 5 | 20 | 30 | 35
Proving Constant (1 Dial Division = 2.89 N) | 2.89 | 2.89 | 2.89 | 2.89 | 2.89 | 2.89
Axial force (P) (in N) | 0 | 8.67 | 14.45 | 57.8 | 86.7 | 101.15
Axial Stress=P/Ac (in N/cm2) | 0 | 0.739638 | 1.215609 | 4.814498 | 7.216611 | 8.407394
Axial Stress (in kPa) | 0 | 7.396384 | 12.15609 | 48.14498 | 72.16611 | 84.07394

## Slide 134
Chart: UCC Test
| 0 | 5.2631578947368416 | 6.5789473684210495 | 7.5 | 7.5657894736842106 | 7.6973684210526434
 | 0 | 7.3964 | 12.1561 | 48.145 | 72.1661 | 84.0739

## Slide 135
UCC Strength (kPa) | 84.073941
Undrained Cohesion, Cu (kPa) | 42.036971
Net Safe Bearing Capacity, (qns) | 84.073941
Unit weight of Soil (kN/m3) | 16
Depth of foundation, m | 2.5
Safe Bearing Capacity, (qs) in kPa | 124.07394
Safe Bearing Capacity, (qs) in t/m2 | 12.6

## Slide 136
SOIL EXPLORATION/ SOIL INVESTIGATION
The field and laboratory investigation studies carried out for the necessary information about the sub-soil characteristics including the position of ground water table are termed as SOIL EXPLORATION.
GEOTECHNICAL INVESTIGATIONS

## Slide 137
Leaning Tower of PISA

## Slide 142
MAIN COMPONENTS OF
SUBSURFACE INVESTIGATIONS

## Slide 144
STATIC | DYNAMIC
INDEX CONSISTENCY PERMEABILITY COMPRESSIBILITY COMPACTION STRENGTH TESTS [UCS,COMPRESSION, TENSILE,BRAZILIAN] SHEAR STRENGTH TESTS [DIRECT, TRIAXIAL, VANE] ULTRASONIC PULSE VELOCITY DILATANCY SLAKE DURABILITY | RESONANT COLUMN TEST CYCLIC TRIAXIAL TEST
LABORATORY INVESTIGATIONS

## Slide 145
Planning of SOIL EXPLORATION/
SOIL INVESTIGATION Programme
Reconnaissance
Preliminary Investigation
Detailed Investigation

## Slide 150
Soil Stress & Deformation

## Slide 156
IS 13063 (1991): Code of practice for structural safety of buildings on shallow foundations on rocks [CED 48: Rock Mechanics]

## Slide 157
IS 13063 (1991): Code of practice for structural safety of buildings on shallow foundations on rocks [CED 48: Rock Mechanics]

## Slide 158
Methods of SOIL EXPLORATION/
SOIL INVESTIGATION

## Slide 159
Methods of SOIL EXPLORATION/
SOIL INVESTIGATION

## Slide 160
I. DIRECT METHODS OF SOIL INVESTIGATION
(TEST PITS)

## Slide 161
TRIAL PIT

## Slide 162
II. SEMI-DIRECT METHODS OF SOIL INVESTIGATION
(BORINGS)

## Slide 167
Bulb Auger for Sandy Soils
Hand Operated Augers

## Slide 168
Helical Auger
Hand Operated Augers

## Slide 173
Rock Core Drilling

## Slide 175
FIELD (in-situ) TESTS
Penetration Tests:
Standard Penetration Test (SPT)
Cone Penetration Tests (CPTs)
2. Plate Load Test
3. Pressure Meter Tests

## Slide 176
SAMPLING
1. AUGERS
2. BOREHOLES (A) DIAMOND DRILLING (B) PERCUSSION DRILLING
TESTING | 
STATIC | DYNAMIC
SPT CPT PLATE LOAD TEST PILE LOAD TEST PRESSUREMETER TEST PUMPING TEST CROSS-HOLE TEST BOREHOLE DEFORMATION TEST CABLE JACKING LARGE DIRECT SHEAR TEST | DCT BLOCK VIBRATION TEST PIEZOCONE PENETRATION (CPTU) MARCHETTI DILATOMETER TEST (DMT)
MEASUREMENTS
1. IN-SITU STRESSES
2. DISPLACEMENTS SUBSIDENCES 4. TILTS/ SWAYS
IN –SITU INVESTIGATIONS

## Slide 177
Standard Penetration Test (SPT)

## Slide 178
https://youtu.be/TIaBRn6J1eo?si=DSZp5oBbi2z334

## Slide 184
Donut Hammer

## Slide 195
Chart: Width of Footing, B (in meter)
| 1 | 2 | 3 | 4 | 5 | 6
N=5 | 59.2 | 34.7 | 28.2 | 25.3 | 23.6 | 22.5
N=10 | 207 | 121.5 | 98.8 | 88.5 | 82.6 | 78.8
N=20 | 502.8 | 295.1 | 240 | 214.9 | 200.6 | 191.3
N=30 | 798.5 | 468.7 | 381.2 | 341.3 | 318.5 | 303.9
N=40 | 1094.3 | 642.2 | 522.3 | 467.7 | 436.5 | 416.4
N=50 | 1390 | 815.8 | 663.5 | 594.1 | 554.5 | 529
N=60 | 1685.8 | 989.4 | 804.7 | 720.5 | 672.5 | 641.5

## Slide 196
Rotary Boring carrying using barge

## Slide 197
Cone Penetration Test (CPT)

## Slide 198
https://youtu.be/EepT6mP6VN4?si=J7kUth2o-lRa587k

## Slide 201
SAMPLE DISTURBANCE

## Slide 209
Foundation Types

## Slide 210: Shallow Foundations
bed rock
firm ground
~ for transferring building loads to underlying ground
~ mostly for firm soils or light loads

## Slide 212: Deep Foundations
bed rock
weak soil
P
I
L
E
~ for transferring building loads to underlying ground
~ mostly for weak soils or heavy loads

## Slide 213
Foundation Design
Case study

## Slide 251
CE190423/11
REPORT ON
PLATE LOAD TESTS [K VALUE & SBC]
FOR RAW WATER TANK STRUCTURE (IN NEW WTP)
LOCATION:
PEDDAVARAM VILLAGE,
NANDIGAMA MANDAL,
NTR DISTRICT, ANDHRA PRADESH.
CLIENT:
M/s CRUX BIOETHANOL INDIA PRIVATE LIMITED
TEST CONDUCTED BY:
M/s STANDARD FOUNDATIONS
VIJAYAWADA
DEPARTMENT OF CIVIL ENGINEERING
V.R. SIDDHARTHA ENGINEERING COLLEGE
VIJAYAWADA-520 007
Case study

## Slide 252
Report on PLATE LOAD TESTs for Modulus of Subgrade Reaction value and SBC FOR RAW WATER TANK STRUCTURE
(IN NEW WTP)
REPORT ON
PLATE LOAD TESTS [K-VALUE & SBC]
FOR RAW WATER TANK STRUCTURE (IN NEW WTP)
[PLATE LOAD TESTs]
INTRODUCTION:
M/s CRUX BIOETHANOL INDIA PRIVATE LIMITED requested the Civil Engineering
Department of V.R. Siddhartha Engineering College, Vijayawada to conduct PLATE
LOAD TESTS [Part-1] for the estimation of Modulus of Subgrade Reaction value and
SBC value [K-value] and Safe Bearing Capacity for Raw water Tank area below 1.50
meter in connection with construction of Raw water tank structure (in new WTP) at
PEDDAVARAM VILLAGE, NANDIGAMA MANDAL, NTR DISTRICT, ANDHRA
PRADESH.
MODULUS OF SUB GRADE REACTION (K-VALUE)
- PLATE LOAD TEST:
The Load Test is conducted at the test section of for Raw water Tank area below 1.50
meter in (in new WTP) at PEDDAVARAM VILLAGE, NANDIGAMA MANDAL,
NTR DISTRICT, ANDHRA PRADESH. The Load test was done as per IS: 9214-1971
specifications.

## Slide 253
Report on PLATE LOAD TESTs for Modulus of Subgrade Reaction value and SBC FOR RAW WATER TANK STRUCTURE
(IN NEW WTP)
The Size of the plate will be 750 mm diameter circular plate and 30 mm thick.
The test was conducted 20.04.2023.
The reaction for the vertical compression load test on the plate was obtained by
means of Loaded Vehicle - JCB supported clears of the test plate. The load was applied by
means of hydraulic Jack through beam of the loaded vehicle. The settlements were
recorded by means of three dial gauges of sensitivity 0.01 mm placed on immovable
supports uniformly spaced at 120 degrees. The load was applied by means of hydraulic
jack and the reaction to the jack was provided by loaded vehicle. In between the beam and
jack, Proving Ring of 10000 kgf capacity is placed for the measurement of load and
pressure as per IS: 9214 -1979. [Refer Figure 1 for the arrangement].
The settlements were recorded by means of three dial gauges of sensitivity of 0.01
mm placed on immovable supports placed 2.0 m from the test plate. The test was carried
out by Method II as specified by IS: 9214-1979.
The test bearing plate is first seated by applying a load of 310 kgf equivalent to a
pressure of 0.07 kgf/cm² (7kPa) and released it after few seconds. The deflection dial
gauges and the proving ring dial gauge are set to read Zero. Then a load sufficient to
cause approximately 0.25 mm settlement is applied and when there is no appreciable
increase in settlement (when the rate of change of increase in settlement is less than
0.025 mm/ min.), the readings of the three-deflection dial gauges are recorded. The
load as measured by the proving ring is also recorded.

## Slide 254
Report on PLATE LOAD TESTs for Modulus of Subgrade Reaction value and SBC FOR RAW WATER TANK STRUCTURE
(IN NEW WTP)
The load is increased with an additional settlement of approximately 0.25 mm. The load and
deflections are recorded. This procedure is repeated until a total settlement of not less than
1.75 mm has been produced. The results obtained from the load test are presented in Table-
1.
Computation of K value from the load test:
Generally, the Modulus of Subgrade Reaction value and SBC is proportional to the
deflection ie the pressure - deflection relationship is linear. K value will be the slope of this
linear relationship.
K-value = p /0.125 in kgf/cm²/cm- (1)
Where, p = pressure load intensity corresponding to deflection of plate of 1.25 mm
The following corrections are applied before a final value of Sub grade reaction "K" is
evaluated.
1. Correction when using plates smaller than 750 mm diameter
2. Correction of Load - Deflection Curve - This correction should be necessary if
the value of Ku is 5.55 kg/cm²/cm or more.
3. Correction for Bending of the plates.
4. Corrections for saturation
A graph between Load and the settlement of the plate was drawn (Figure-2) to assess the
Modulus of Sub Grade Reaction, K-value. The relationship is Linear and shear failure.
Load corresponding to 1.25 mm settlement
= 6700 kgf
Ku-Value [uncorrected] = [6011.905 / (4418.4375 x 1.107)] = 12.295 kgf/cm²/cm
K-Value after correction = [ 6700 / (4418. 4375 x 0.125)] = 12.131 kgf/cm²/cm
Hence, a modulus sub grade reaction, K value of 12.131 kgf/cm²/cm is recommended
for Raw water Tank area below 1.50 meter in connection with construction of Raw water
tank structure (in new WTP) at PEDDAVARAM VILLAGE, NANDIGAMA
VILLAGE, NTR DISTRICT, ANDHRA PRADESH.

## Slide 255
Report on PLATE LOAD TESTs for Modulus of Subgrade Reaction value and SBC FOR RAW WATER TANK STRUCTURE
(IN NEW WTP)
PLATE LOAD TEST: [SBC]
The Load Test is conducted at the test section of for Raw water Tank area below 1.50
meter in connection with construction of Raw water tank structure (in new WTP) at
PEDDAVARAM VILLAGE, NANDIGAMA VILLAGE, NTR DISTRICT, ANDHRA
PRADESH.
The Plate Load test was done as per IS: 1888-1982. The Size of the plate will be 300 mm
x 300 mm x 25 mm thick. The test was conducted on 18.04.2023.
The reaction for the vertical compression load test on the plate was obtained by
means of loaded dead weight Kentledge - JCB supported. The load was applied by means of
JCB. The settlements were recorded by means of two dial gauges of sensitivity 0.01 mm
placed on immovable supports. The load was applied by means of hydraulic jack and the
reaction to the jack was provided by means of JCB beam.
The settlements were recorded by means of two dial gauges of sensitivity of 0.01 mm
placed on immovable supports placed 1.50 m from the test plate. The test was carried out by
applying a series of vertical downward incremental loads of approx. 1.40 tonnes. The
displacements in each loading stage were measured till the rate of displacement of the plate
as stipulated by the code. The load was maintained by least 15 minutes.
The results obtained from the load test are presented in Table-2. The plate is loaded
up to failure or up to the load corresponding to 25/ 50 mm total settlement.

## Slide 256
Report on PLATE LOAD TESTs for Modulus of Subgrade Reaction value and SBC FOR RAW WATER TANK STRUCTURE
(IN NEW WTP)
The Plate was loaded up to 19.60 tonnes and the corresponding total settlement was
found to be 10.47 mm. The load was maintained for a period of 1 hour and then the plate
was unloaded. A graph between applied load and the settlement was drawn (Figure-3 and 4)
to assess the ultimate bearing capacity of soil and design of foundation for a
given settlement.
SAFE BEARING CAPACITY OF SOIL
Size of the Plate -300 mm x 300 mm
The following relationship for the settlement is used to find the settlement of the plate
as per IS: 1888-1982 for a given Size of the foundation
푺 =푺 [푩 (푩 +0.3)/ 푩 (푩 +0.3)]2
풓
풑
풓
풑
풑
풓
It is possible to identify the ultimate load from the Load Vs Settlement curve. The shape of
the curve indicates the soil condition. The Curve comes under "D" type curve for Dense
cohesionless soil as per IS: 1888:1982 In cases where yield point is not well defined,
settlements shall be plotted as abscissa against corresponding load intensities as ordinate,
both to logarithmic scales, which give two straight lines, the intersection of which shall be
considered as yield value.
Dr. G.V. Rama Subba Rao
Associate Professor

## Slide 259
Report on PLATE LOAD TESTs for Modulus of Subgrade Reaction value and SBC FOR RAW WATER TANK STRUCTURE
(IN NEW WTP)
CE190423/11
CONCLUSIONS:
Based on the load tests data for Raw water Tank area below 1.50 meter in connection
with construction of Raw water tank structure (in new WTP) at PEDDAVARAM
VILLAGE, NANDIGAMA VILLAGE, NTR DISTRICT, ANDHRA PRADESH, the
following recommendations are made:
 The Modulus of Sub Grade Reaction load test results are presented in Table 1.
 The Load Vs Plate deflection curve is given in Figure 2.
 The load-deflection curve is linear and General Shear failure.
 A modulus sub grade reaction, K - value of 12.131 kgf/cm²/cm is recommended
for the for Raw water Tank area below 1.50 meter in connection with construction
of Raw water tank structure (in new WTP) at PEDDAVARAM VILLAGE,
NANDIGAMA VILLAGE, NTR DISTRICT, ANDHRA PRADESH.
 The Plate load test results are presented in Table 2.
 The Load Vs Plate Settlement curve is given in Figure 3 and 4.
 The shape of the load -settlement belongs to "D" as per IS: 1888:1982
 From the load settlement relationship on log-log scale an ultimate load of 8.00
tonnes is proposed.
 A safe bearing capacity of 29.67 t/m² [ 296 kN/m²] is proposed for Raw water
Tank area below 1.50 meter in connection with construction of Raw water tank
structure (in new WTP) at PEDDAVARAM VILLAGE, NANDIGAMA
VILLAGE, NTR DISTRICT, ANDHRA PRADESH.
Dr. G.V. Rama Subba Rao
Associate Professor
Professor & HOD-CIVIL
DEAN/Principal

## Slide 264
Case study

## Slide 272: Retaining Walls
~ for retaining soils from spreading laterally
Road
Train
retaining wall
Earth Retaining Structures

## Slide 276
Case study

## Slide 277
CONTIGUOUS PILE WALL AS DEEP EXCAVATION SUPPORTING SYSTEM AT A COMMERCIAL COMPLEX IN VIJAYAWADA, ANDHRA PRADESH, INDIA- CASE HISTORY
A supporting system for proposed 11.2m deep excavation was necessary for a commercial complex at Vijayawada, India. The planning of sub-soil has been carried as per the Indian standard codal provisions [12]. Five bore holes of 25m deep are taken in such a way that one at centre and one at each corner of the site. Average profile and properties of soil layers are evaluated as per Indian standard soil laboratory testing and classification procedures [13, 14] and are presented in Fig. 10. Presence of footings of adjacent buildings and underground utilities were some of the decisive factors that eliminated choice of diaphragm wall for supporting the excavation. In this situation, contiguous pile wall for supporting the excavation is the right the choice.

## Slide 278
Detailed lateral earth pressures acting on the wall are calculated and shown in Fig. 11 Stability analysis of the wall has been carried to evaluate the depth of penetration (DP) by equating active force on right side of the wall to passive force on left side of the wall. For the present case, DP is 5.64m. By applying factor of safety of 1.5 to coefficient of passive earth pressure, DP is 7.79m. An actual penetration depth (DP) of 9.8m (=1.25x7.79m) is adopted. The factor of safety against sand boiling is 5.16 obtained by using equation (1) with consideration of sand layer throughout the penetration depth. This value is greater than 1.5. Hence, wall is stable against sand boiling also.
The diameter of pile used is 600mm. M30 grade concrete and Fe500 grade steel are used for making each pile. For contiguous piles, the c/c spacing is used for estimating reinforcement quantity. The pile is designed to resist the moment caused by the lateral earth pressure. The pile is designed to resist a maximum bending moment of 726.82 kN-m. This moment is evaluated from deducting moment due to the active force and moment due to the passive force with respect to pile bottom. Area of reinforcement required for the pile section is 10,179 mm2 which can be obtained from Indian standard design aids [15]. A clear cover of 50mm provided to the pile section. The required area of main reinforcement is satisfied by providing 14 bars of 32mm diameter. The strength of the core concrete is enhanced by the confinement through spiral (helical) reinforcement [16, 17]. Therefore, helical reinforcement of 8mm Diameter and 50mm Pitch are provided. Reinforcement details are presented in the Fig. 12.

## Slide 279
The pile wall comprised 600mm diameter bored cast-in-situ piles spaced at 0.7m c/c, with an average embedment depth of 9.8m. These shall be installed vertically along the proposed line of excavation. These piles were designed as cantilever retaining system without provision of anchors. Capping beam of 1200 x 750mm size was cast along the alignment of the pile which was designed to take care of differential changes in the earth pressures in the adjacent piles. The peripheral length of excavation was 310m and 442 piles were involved in the support work. Individual piles were constructed in the same way as a typical Bored Cast-in-situ piles using temporary casings and bentonite slurry.
Excavation operations proceeded only in those areas where pile concrete attained maturity. General construction sequence for the piling operation is: (i) Centering of rotary rig on the proposed pile point (ii) Carrying out the boring operation upto the upto about 21m below the existing ground level (iii) Driving the casing if needed (iv) Maintaining the stability of the borehole simultaneously with bentonite slurry (v) Continuing boring operation in soil using soil bucket and/or Soil auger depending on the stratum (vi) After completion of boring, cleaning of borehole by bentonite flushing (vii) Lowering of reinforcement cage into the borehole (viii) Repeat bentonite flushing operation and subsequently (ix) Pouring M30 grade concrete through tremie. The water drained out shall be let away from the site such that it does not re-enter in to the site. If ground water table is encountered in the region of operation, then suitable well point dewatering system should be activated to avoid flooding and subsequent collapse. Plate 1 shows the contiguous pile wall constructed at the site.

## Slide 281
Fig. 11 Lateral Earth Pressures acting on the Wall

## Slide 284
Case study

## Slide 285
Sir ARTHUR THOMAS COTTON

## Slide 286: Prof. Dr. P.V. Narasaiah garu

## Slide 287: Prof. Dr. K. Mallikarjuna Rao garu, SVU

## Slide 289
Thank You one and all